## Slide 1: Machine Learning Framework for Impurity Level Prediction in Semiconductors
Arun Mannodi-Kanakkithodi✢, Michael Toriyama✢, Fatih G. Sen✢, Michael J. Davis✵, Maria K.Y. Chan✢ ✢Center for Nanoscale Materials, Argonne National Laboratory
✵Chemical Sciences and Engineering, Argonne National Laboratory

## Slide 2: Overview
In this Tutorial, we will follow a fairly standard workflow in AI applications in Science. The problem involves generating a mapping from a set of descriptors X to a set of properties P using machine learning. The steps typically include:
Find raw data from experiments or simulations (or both).
Extract relevant information from the raw data.
Generate descriptors X – try to check which of the descriptors are relevant and which are not with a goal of getting a minimal set of relevant descriptors (dimensional reduction).
Select a machine learning model that may be appropriate for the problem.
Set up a scheme to train the model on some subsets of the data, and use other subsets for validation.
Tweak the model to optimize it, maybe check other models to see if they work better.
Make predictions outside the training and validation domain.
In the particular case here, the problem involves defect levels in semiconductors, which is relevant for photovoltaics and optical absorption. However, the workflow is rather generic and applies broadly.
The data were in this case generated using atomistic density functional theory calculations, and there are some additional data points generated for checking how the final machine learning model works outside the training and validation sets.

## Slide 3: Impurity Levels in Semiconductors
Experimental
Sample preparation difficult with DLTS or CL.
Difficult to assign observed levels to particular defect.
Density Functional Theory (DFT)
Large supercells, charge states  expensive.
Prior knowledge not utilized for new defect levels.
CHALLENGES

## Slide 4: Predicting Impurity Behavior in Semiconductors
Semiconductor + impurity
“Computational Study of Pb Substitution in MAPbBr3”, Chem. Mater. (2019).
"Machine-learned impurity level prediction for Cd chalcogenides”, npj Comput. Mater. (2020).
“Impurity Level Prediction and Screening in Halide Perovskites using Machine Learning”, in prep.
Density Functional Theory
Ef(q) = E(Dq) – E(bulk) + ∑niµi + q(EF+Evbm) + Ecorr
Impurity levels: 𝜀(q1/q2) = [ Ef(q1) - Ef(q2) ] / (q2-q1)
-1/-2
+2/+1
Impurity levels 𝜀(q1/q2):
Fermi energies (EF) where defect transitions from one stable charge state (q1) to another (q2)
Expensive DFT Computation
ML prediction On-demand
Descriptors (X)
Elemental properties
Coordination environment
Unit cell defect calculations
Machine Learning
Linear correlation coefficients between X and P
Regression (eg. random forest) model  P = f(X)
Main DFT output: Defect formation energy (enthalpy) and charge transition level (the chemical potential at which a defect changes charge state)

## Slide 5: DFT Dataset for Machine Learning
CdX | Doping Site | M | ∆H(Cd-rich) | ∆H(Mod) | ∆H(Te-rich) | (+3/+2) | (+2/+1) | (+1/0) | (0/-1) | (-1/-2) | (-2/-3)
CdTe | M_Te | N | 2.09 | 2.48 | 2.88 | -0.97 | -0.67 | -0.40 | -0.08 | 1.44 | 1.90
CdTe | M_Te | O | 1.17 | 1.17 | 1.43 | -0.91 | -0.65 | -0.33 | 0.95 | 1.37 | 2.11
CdTe | M_i_Te_site | Rh | 3.46 | 3.93 | 4.88 | -0.52 | 0.05 | 0.56 | 1.12 | 1.83 | 2.14
CdTe | M_Te | Re | 6.75 | 7.22 | 7.70 | 0.68 | -0.49 | -1.05 | 0.61 | 1.72 | 2.18
CdSe | M_Se | Si | 2.59 | 3.27 | 5.21 | -0.64 | -0.33 | 0.30 | 0.70 | 1.10 | 2.21
CdTe | M_Cd | Be | 0.58 | 0.46 | 0.34 | -0.92 | -0.65 | -0.32 | 1.40 | 1.84 | 2.22
CdTe | M_i_Cd_site | F | 1.72 | 1.48 | 1.24 | -0.85 | -0.56 | -0.29 | 0.03 | 1.77 | 2.23
CdTe | M_i_Te_site | F | 2.61 | 2.38 | 2.14 | -0.84 | -0.51 | -0.22 | 0.09 | 1.80 | 2.26
CdSe | M_Cd | Cu | 2.49 | 1.23 | 1.05 | -0.88 | -0.51 | -0.14 | 0.36 | 1.79 | 2.33
CdSe | M_Se | Os | 5.88 | 6.53 | 7.17 | -0.55 | -0.55 | 0.05 | 1.44 | 1.90 | 2.36
CdSe | M_i_Cd_site | F | 1.95 | 1.63 | 1.31 | -0.83 | -0.51 | -0.21 | 0.12 | 1.82 | 2.38
CdTe | M_i_Cd_site | Hg | 1.78 | 1.47 | 1.76 | -0.65 | -0.15 | 0.29 | 1.66 | 2.06 | 2.42
CdTe | M_i_old | Cu | 2.50 | 1.94 | 2.22 | -0.74 | -0.40 | 1.26 | 1.72 | 2.08 | 2.43
CdSe | M_i_Se_site | Cl | 3.68 | 3.36 | 3.03 | -0.65 | -0.32 | 0.05 | 0.38 | 1.94 | 2.51
CdTe | M_Cd | Sr | 1.06 | 1.06 | 1.06 | -0.64 | -0.41 | -0.10 | 1.66 | 2.11 | 2.52
CdS | M_i_S_site | S | 5.23 | 4.57 | 3.91 | -0.06 | -0.05 | 0.78 | 1.13 | 1.59 | 2.69
CdS | M_i_Cd_site | S | 4.81 | 4.15 | 3.49 | -0.56 | -0.27 | 0.56 | 1.02 | 1.50 | 2.71
CdS | M_Cd | O | 7.52 | 6.22 | 5.56 | -0.87 | -0.30 | 0.10 | 0.47 | 2.11 | 2.75
CdS | M_i_old | S | 4.65 | 3.99 | 3.33 | -0.65 | 0.83 | 0.83 | 1.48 | 1.95 | 2.75
CdSe | M_i_Se_site | Pd | 2.22 | 1.58 | 2.02 | -0.62 | -0.19 | 0.27 | 1.56 | 2.09 | 2.89
CdS | M_Cd | S | 6.04 | 4.73 | 3.42 | -0.80 | 0.46 | 0.83 | 1.32 | 2.32 | 2.94
CdSe | M_Cd | Pb | 0.76 | 0.73 | 0.74 | -0.68 | -0.16 | 0.34 | 1.67 | 2.19 | 2.97
CdS | M_i_old | Pt | 3.03 | 2.38 | 3.25 | -0.43 | 0.23 | 0.72 | 1.98 | 2.57 | 3.38
CdS | M_S | Se | 0.19 | 0.20 | 0.21 | -0.77 | -0.42 | -0.12 | 1.95 | 2.53 | 3.39
Dataset 1: Formation Enthalpies (∆H)  945 impurities  945 points (each)
Dataset 2: Charge Transition Levels (𝜀(q1/q2))  381 impurities  2286 points (combined)

## Slide 6
Root mean square error (RMSE) between DFT and experiments
= 0.22 eV
ML models with similar accuracy can replace DFT computations and lead to accelerated screening.
𝜀(q1/q2): DFT vs Experiments
CdTe
"Machine-learned impurity level prediction for Cd chalcogenides”, npj Comput. Mater. (2020).

## Slide 7
Correlation between descriptors & properties
Descriptors from unit cell defect calculations show largest correlations.
Unit cell defect VBM & CBM have > 80% correlation with +1/0 & -1/0 transition levels.
Unit cell defect ∆H is 90% correlated with supercell ∆H.
Unit cell defect calculation
Elemental properties of M
DATASET: ~ 400 impurities in CdTe, CdSe and CdS.
Impurity simulated in an 8 atom unit cell; two orders of magnitude cheaper calculation

## Slide 8: Descriptors for Machine Learning
CdX | Doping Site | M | Delta Ion. En. | Delta At. Rad. | Delta EN | Delta Val. | … | Unit_cell_def CBM | Unit_cell_def ∆H(Mod) | Unit_cell_def ∆H(X-rich)
CdTe | M_Te | N | -347.5 | 0.061 | -0.71 | -1 |  | 1.156 | 1.048 | 0.812
CdTe | M_Te | O | -371.9 | 0.411 | -0.76 | -1 |  | 1.316 | 1.173 | 1.083
CdTe | M_i_Te_site | Rh | -448.9 | 0.861 | -0.87 | -1 |  | 1.647 | 1.942 | 1.965
CdTe | M_Te | Re | -464.7 | 0.991 | -0.87 | 2 |  | 2.140 | 2.326 | 2.481
CdSe | M_Se | Si | -492 | 1.181 | -0.9 | -1 |  | 2.000 | 3.000 | 3.000
CdTe | M_Cd | Be | 31.7 | -0.369 | -0.12 | 0 |  | 2.718 | 0.770 | 0.651
CdTe | M_i_Cd_site | F | -130 | 0.111 | -0.38 | 0 |  | 2.907 | 0.113 | 0.114
CdTe | M_i_Te_site | F | -277.9 | 0.481 | -0.69 | 0 |  | 2.995 | 0.864 | 0.865
CdSe | M_Cd | Cu | -318.2 | 0.661 | -0.74 | 0 |  | 2.995 | 1.276 | 1.277
CdSe | M_Se | Os | -364.8 | 0.731 | -0.8 | 0 |  | 2.897 | 1.807 | 1.808
CdSe | M_i_Cd_site | F | -67.1 | -0.509 | 0.35 | 1 |  | 3.300 | 3.320 | 2.846
CdTe | M_i_Cd_site | Hg | -290.1 | -0.059 | -0.08 | 1 |  | 3.547 | 0.954 | 1.214
CdTe | M_i_old | Cu | -288.9 | -0.079 | 0.12 | 1 |  | 3.032 | 0.757 | 0.856
CdSe | M_i_Se_site | Cl | -309.4 | 0.171 | 0.09 | 1 |  | 3.327 | 0.723 | 0.920
CdTe | M_Cd | Sr | -278.4 | 0.221 | 0.35 | 1 |  | 2.854 | 0.999 | 0.796
CdS | M_i_S_site | S | 218.7 | -0.579 | 0.86 | 2 |  | 3.506 | 5.499 | 5.025
CdS | M_i_Cd_site | S | -81.3 | -0.169 | 0.21 | 2 |  | 3.408 | 1.755 | 1.281
CdS | M_Cd | O | -105.6 | -0.119 | 0.32 | 2 |  | 3.541 | 0.897 | 0.737
CdS | M_i_old | S | -159.1 | 0.131 | 0.27 | 2 |  | 3.491 | 1.076 | 1.077
CdSe | M_i_Se_site | Pd | -152.2 | 0.261 | 0.64 | 2 |  | 3.457 | 0.980 | 0.981
CdS | M_Cd | S | 534.6 | -0.569 | 1.35 | 3 |  | 2.140 | 4.523 | 3.970
CdSe | M_Cd | Pb | 144 | -0.209 | 0.5 | 3 |  | 2.945 | 2.574 | 2.045
CdS | M_i_old | Pt | 79.3 | -0.099 | 0.47 | 3 |  | 3.116 | 1.953 | 1.502
CdS | M_S | Se | -34 | 0.101 | 0.36 | 3 |  | 3.375 | 4.104 | 4.342
Descriptor Set 1: Elemental Properties (14 features)
Descriptor Set 2: Unit Cell Defect Properties (5 features)
Descriptor Set 3: Elemental + Unit Cell (19 features)

## Slide 9
Steps Involved in Training a Material  Property Regression Model
READ DATA: Labels, computed properties, descriptors.
SELECT ML TECHNIQUE: Random Forest / Kernel Ridge / LASSO / etc.
TRAIN DEFAULT MODEL: With a (for eg.) 70-30 training-test split, train a model using chosen technique.
HYPERPARAMETER OPTIMIZATION: Improve model by tuning every hyperparameter to minimize test prediction error.
CROSS-VALIDATION: Divide training data into n folds, tune hyperparameters to minimize cross-validation test error.
LEARNING CURVES: Model prediction performance vs training set size.
DEPLOY BEST MODEL: Make new predictions and discovery.

## Slide 10
Random Forest: Formation Enthalpy
Models trained for ∆H (Cd-rich) on CdTe+CdSe+CdS data
Elemental properties + unit cell defect properties lead to best models.
"Machine-learned impurity level prediction for Cd chalcogenides”, npj Comput. Mater. (2020).

## Slide 11
∆H (Cd-rich) (eV)
∆H (X-rich) (eV)
CdTe
CdSe
CdS
Random Forest: Formation Energy
RMSE
Training: 0.30 eV
Test: 0.40 eV
Outside: 0.55 eV

## Slide 12
Random Forest: Impurity Levels
Models trained for 𝜀(q1/q2) on CdTe+CdSe+CdS data
Elemental properties + unit cell defect properties lead to best models.
"Machine-learned impurity level prediction for Cd chalcogenides”, npj Comput. Mater. (2020).

## Slide 13
Random Forest: Transition Levels
CdTe
CdSe
CdS
Test RMSE:
0.30 eV
Outside RMSE:
0.35 eV
RF Model to predict 𝜀(q1/q2) (eV)
Out-of-sample prediction

## Slide 14
Impurity Formation Energies:
DFT vs ML
ML models trained on dataset of 381 impurities in CdTe, CdSe & CdS are used to predict complete formation energies for 1827 impurities in 5 compounds; in theory applicable to any impurity in any Cd-Te-Se-S compound.

## Slide 15: Acknowledgements
LCRC
CONTACT: mannodiarun@anl.gov
Argonne LDRD: Office of Science #DE-AC02-06CH11357
EERE PVRD: SunShot program #DOE DEEE005956.

## Slide 16: THANK YOU